RINA AH36, RINA AH36 steel grade, RINA AH36 steel plate, RINA AH36 steel sheet, RINA AH36 shipbuilding steel price,RINA AH36 steel supplier and manufacturer.

RINA AH36 shipbuilding Steel Description:
RINA AH36 steel is a kind of  high tensile strength marine steel. All of these steels have been engineered to be optimal long-lived shipbuilding steels.As with other grades of steel, they have a specific gravity of 7.8. Higher-strength RINA shipbuilding steel comes in 12 grades of 3 strengths, AH36 is one of the grades. The RINA AH36 grades have yield strength of 51,000 psi (355 MPa), and ultimate tensile strength of 71,000 - 90,000 psi (490-620 MPa). All the RINA AH36 shipbuilding Steel offered by Ice steel can be certificated by Registro Italiano Navale (RINA) as per customer’s request.

RINA AH36 Shipbuilding Steel Application:
RINA AH36 Shipbuilding steel plates are mainly used for making the offshore oil drilling platform, the hull of ship building and ship repairing, the platform pipe joints and other components. RINA AH36 Shipbuilding steel plates also can be used for producing container and bulk cargo vessels as well as cruise ships, ferries and yachts.

RINA AH36 Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

RINA AH36 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RINA Grade AH36 | 0.180 | 0.1-0.5 | 0.90-1.6 | 0.035 | 0.035 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % |  |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.400 | 0.020 |  |  |  |

RINA AH36 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| RINA Grade AH36 | 8mm-50mm | Min 355Mpa | 490-620Mpa | 21% | -0 | 34J |
|  | 51mm-70mm | Min 355Mpa | 490-620Mpa | 21% | -0 | 41J |
|  | 71mm-100mm | Min 355Mpa | 490-620Mpa | 21% | -0 | 50J |
| The min impact energy is longitudinal energy |

BeiJing ICE iron and steel co., Ltd. is a professional steel company in manufacturing and exporting RINA AH36 shipbuilding steel plates and sheets. Our RINA AH36 steel plates have been exported to worldwide shipyard and ship building company.If you have any needs in RINA Grade AH36 steel plate price, please feel free to contact us.