RINA AH40, RINA AH40 steel grade, RINA AH40 steel plate, RINA AH40 steel sheet, RINA AH40 shipbuilding steel price,RINA AH40 steel supplier and manufacturer.

RINA AH40 shipbuilding Steel Description:
RINA AH40 steel is a kind of  high tensile strength shipbuilding steel. All RINA AH40 steels are standard hot rolled carbon steels. All of these steels have been engineered to be optimal long-lived shipbuilding steels. Higher-strength RINA shipbuilding steel comes in 12 grades of 3 strengths, AH40 is one of the grades.

RINA AH40 Shipbuilding Steel Application:
RINA AH40 Shipbuilding steel plates are mainly used for making the offshore oil drilling platform, the hull of ship building and ship repairing, the platform pipe joints and other components.

RINA AH40 Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

RINA AH40 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RINA Grade AH40 | 0.180 | 0.1-0.5 | 0.90-1.6 | 0.035 | 0.035 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % |  |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.400 | 0.020 |  |  |  |

RINA AH40 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| RINA Grade AH40 | 8mm-50mm | Min 390Mpa | 510-650Mpa | 20% | 0 | 34J |
|  | 51mm-70mm | Min390Mpa | 510-650Mpa | 20% | 0 | 41J |
|  | 71mm-100mm | Min 390Mpa | 510-650Mpa | 20% | 0 | 50J |
| The min impact energy is longitudinal energy |

BeiJing ICE iron and steel co., Ltd. is a professional RINA AH40 steel manufacturer and exporter. Our RINA AH40 steel plates and steel sheets have been exported to worldwide shipyard and ship building company.If you have any needs in RINA Grade AH40 steel plate price, please feel free to contact us.