RINA DH36, RINA DH36 steel grade, RINA DH36 steel plate, RINA DH36 steel sheet, RINA DH36 shipbuilding steel price,RINA DH36 steel supplier and manufacturer.

RINA DH36 Shipbuilding Steel Description:
RINA DH36 steel is a kind of  high tensile strength marine steel. Higher-strength RINA shipbuilding steel comes in 12 grades of 3 strengths, DH36 is one of the grades. As with other grades of steel, they have a specific gravity of 7.8. The RINA DH36 grades have yield strength of 51,000 psi (355 MPa), and ultimate tensile strength of 71,000 - 90,000 psi (490-620 MPa). All the RINA DH36 shipbuilding Steel offered by Ice steel can be certificated by Registro Italiano Navale (RINA) as per customer’s request.

RINA DH36 Shipbuilding Steel Application:
RINA DH36 Shipbuilding steel plates are mainly used for making the offshore oil drilling platform, the hull of ship building and ship repairing, the platform pipe joints and other components.

RINA DH36 Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

RINA DH36 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RINA Grade DH36 | 0.180 | 0.1-0.5 | 0.90-1.6 | 0.035 | 0.035 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % |  |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.400 | 0.020 |  |  |  |

RINA DH36 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| RINA Grade DH36 | 8mm-50mm | Min 355Mpa | 490-620Mpa | 21% | -20 | 34J |
|  | 51mm-70mm | Min 355Mpa | 490-620Mpa | 21% | -20 | 41J |
|  | 71mm-100mm | Min 355Mpa | 490-620Mpa | 21% | -20 | 50J |
| The min impact energy is longitudinal energy |

BeiJing ICE iron and steel co., Ltd. has steel mill to produce RINA DH36 shipbuilding steel. ICE Steel is a RINA DH36 steel exporter too. The RINA DH36 shipbuilding steel plates and sheets we made have been exported to worldwide shipyard and ship building company.If you have any needs in RINA Grade DH36 steel plate price, please feel free to contact us.