RINA EH32, RINA EH32 steel grade, RINA EH32 steel plate, RINA EH32 steel sheet, RINA EH32 shipbuilding steel price,RINA EH32 steel supplier and manufacturer.

RINA EH32 shipbuilding Steel Description:
All RINA steels are standard carbon steels. As with other grades of steel, they have a specific gravity of 7.8. Higher-strength RINA shipbuilding steel comes in 12 grades of 3 strengths, EH32 is one of the grades.The RINA EH 32 grade steel plates have yield strength of 45,500 psi (315 MPa), and ultimate tensile strength of 64,000 - 85,000 psi (440-590 MPa).

RINA EH32 Shipbuilding Steel Application:
RINA EH32 Shipbuilding steel plates are mainly used for making the hull of ship building and ship repairing, the offshore oil drilling platform, the platform pipe joints and other components.

RINA EH32 Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

RINA EH32 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RINA Grade EH32 | 0.180 | 0.1-0.5 | 0.90-1.6 | 0.035 | 0.035 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % |  |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.400 | 0.020 |  |  |  |

RINA EH32 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| RINA Grade EH32 | 8mm-50mm | Min 315Mpa | 440-590Mpa | 22 | -40 | 34J |
|  | 51mm-70mm | Min 315Mpa | 440-590Mpa | 22 | -40 | 38J |
|  | 71mm-100mm | Min 315Mpa | 440-590Mpa | 22 | -40 | 46J |
| The minimum impact energy is longitudinal energy |

IC Steel has been working in the steel industry for many years. Ice steel is a professional RINA EH32 shipbuilding steel supplier and exporter. RINA EH32 shipbuilding steel plates and steel sheets provided by Ice steel have been exported to worldwide shipyard and ship building company. If you have any needs in RINA EH32 steel plate price, please feel free to contact us.