RINA EH40, RINA EH40 steel grade, RINA EH40 steel plate, RINA EH40 steel sheet, RINA EH40 shipbuilding steel price,RINA EH40 steel supplier and manufacturer.

RINA EH40 shipbuilding Steel Description:
RINA EH40 steel is a kind of  hot rolled high tensile strength steel. Higher-strength RINA shipbuilding steel comes in 12 grades of 3 strengths, EH40 is one of the grades. The RINA EH40 grade steel plates have yield strength of 56,500 psi (390 MPa), and ultimate tensile strength of 74,000 - 94,500 psi (510-650 MPa).All of RINA EH40 steels have been engineered to be optimal long-lived shipbuilding steels.

RINA EH40 Shipbuilding Steel Application:
RINA EH40 Shipbuilding steel plates are suitable for container and bulk cargo vessels as well as cruise ships, ferries and yachts.

RINA EH40 Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

RINA EH40 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RINA Grade EH40 | 0.180 | 0.1-0.5 | 0.90-1.6 | 0.035 | 0.035 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % |  |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.400 | 0.020 |  |  |  |

RINA EH40 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| RINA Grade EH40 | 8mm-50mm | Min 390Mpa | 510-650Mpa | 20% | -40 | 34J |
|  | 51mm-70mm | Min390Mpa | 510-650Mpa | 20% | -40 | 41J |
|  | 71mm-100mm | Min 390Mpa | 510-650Mpa | 20% | -40 | 50J |
| The min impact energy is longitudinal energy |

BeiJing ICE iron and steel co., Ltd. has many years experience in making RINA EH40 steel. ICE Steel is a very good RINA EH40 steel exporter too. We always provide the RINA EH40 steel in high quality and best price. If you have any needs in RINA Grade EH40 steel plate price, please feel free to contact us.