RINA FH32, RINA FH32 steel grate, RINA FH32 steel plate, RINA FH32 steel sheet, RINA FH32 shipbuilding steel price,RINA FH32 steel supplier and manufacturer.

RINA FH32 shipbuilding Steel Description:
RINA FH32 steel is a kind of  hot rolled high tensile strength steel. RINA FH32 steel can achieve the impact toughness at Celsius degree -60°. The RINA FH 32 grade steel plates have yield strength of 45,500 psi (315 MPa), and ultimate tensile strength of 64,000 - 85,000 psi (440-590 MPa). All the RINA FH32 shipbuilding Steel offered by Ice steel can be certificated by Registro Italiano Navale (RINA).

RINA FH32 Shipbuilding Steel Application:
RINA FH32 Shipbuilding steel plates can be used for producing container and bulk cargo vessels as well as cruise ships, ferries and yachts.RINA FH32 Shipbuilding steel plates are mainly used for making the hull of ship building and ship repairing, the offshore oil drilling platform, the platform pipe joints and other components.

RINA FH32 Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

RINA FH32 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RINA Grade FH32 | 0.160 | 0.1-0.5 | 0.90-1.6 | 0.025 | 0.025 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % | N % |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.800 | 0.020 | 0.009 |  |  |

RINA FH32 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| RINA Grade FH32 | 8mm-50mm | Min 315Mpa | 440-590Mpa | 22% | -60 | 34J |
|  | 51mm-70mm | Min 315Mpa | 440-590Mpa | 22% | -60 | 41J |
|  | 71mm-100mm | Min 315Mpa | 440-590Mpa | 22% | -60 | 50J |
| The min impact energy is longitudinal energy |

Ice steel is a professional RINA FH32 shipbuilding steel supplier and exporter. RINA FH32 shipbuilding steel plates and steel sheets provided by Ice steel have been exported to worldwide shipyard and ship building company. We have steel mill for manufacturing RINA Grade FH32 steel.If you have any needs in RINA FH32 steel plate price, please feel free to contact us.