Grade RINA FH40, RINA FH40 steel, RINA FH40 steel plate, RINA FH40 steel sheet, RINA FH40 shipbuilding steel price,RINA FH40 steel supplier and manufacturer.

RINA FH40 shipbuilding Steel Description:
RINA FH40 steel is a kind of hot rolled high tensile strength steel. The RINA FH40 grade steel plates have yield strength of 56,500 psi (390 MPa), and ultimate tensile strength of 74,000 - 94,500 psi (510-650 MPa). RINA FH40 steel can achieve the impact toughness at Celsius degree -60°. All the RINA FH40 shipbuilding Steel offered by Ice steel can be certificated by Registro Italiano Navale (RINA).

RINA FH40 Shipbuilding Steel Application:
RINA FH40 Shipbuilding steel plates are mainly used for making the offshore oil drilling platform, the hull of ship building and ship repairing, the platform pipe joints and other components.

RINA FH40 Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

RINA FH40 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RINA Grade FH40 | 0.160 | 0.1-0.5 | 0.90-1.6 | 0.025 | 0.025 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % | N% |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.800 | 0.020 | 0.009 |  |  |

RINA FH40 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| RINA Grade FH40 | 8mm-50mm | Min 390Mpa | 510-650Mpa | 20% | -60 | 34J |
|  | 51mm-70mm | Min390Mpa | 510-650Mpa | 20% | -60 | 41J |
|  | 71mm-100mm | Min 390Mpa | 510-650Mpa | 20% | -60 | 50J |
| The min impact energy is longitudinal energy |

BeiJing ICE iron and steel co., Ltd. has many years experience in making every grade shipbuilding steel. We have good quality RINA FH40 steel plates for sale.ICE Steel is a very good RINA FH40 steel exporter too. Our steel plates and steel sheets have been exported to worldwide shipyard and ship building company.If you have any needs in RINA Grade FH40 steel plate price, please feel free to contact us.