RINA Grade B, RINA Grade B steel, RINA Grade B shipbuilding steel, RINA B marine steel plate, RINA B shipbuilding steel sheet, RINA/B steel supplier and manufacturer

RINA Grade B shipbuilding Steel Description:
RINA grade B steel is a kind of hot rolled general tensile strength steel. The RINA B grade steel plates have yield strength of 34,100 psi (235 MPa), and ultimate tensile strength of 58,000 - 75,500 psi (400-520 MPa). RINA steels come 4 grades in ordinary-strength steel for shipbuilding and grade B is one of them.

RINA Grade B shipbuilding Steel Application: 
RINA B Shipbuilding steel plates can be used for ship repairing, the offshore oil drilling platform, the platform pipe joints and other components. RINA B grades of steel plate are almost exclusively used in the Shipbuilding Industry for the construction of structural parts of ships, barges and marine equipment.

RINA Grade B Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

RINA Grade B Shipbuilding Steel Chemical Composition Heat Analysis:

| Element | RINA Grade B Max % | Element | RINA Grade B max % |
| --- | --- | --- | --- |
| C | 0.21 | Ni | - |
| Mn | 0.80 | Mo | - |
| Si | 0.35 | Al | - |
| S | 0.035 | Nb | - |
| P | 0.035 | V | - |
| Cu | - | Ti | - |
| Cr | - | N | - |

RINA B Ship Steel Mechanical Properties:

| Grade | Thickness | Yield Strength | Tensile Strength | Elongation | Impact Energy |
| --- | --- | --- | --- | --- | --- |
|  | (mm) | MPa (min) | MPa | % (min) | (KV J) (min) |
|  |  |  |  |  | 0 degree |
| RINA Grade B | 4-260 | 235 | 400-520 | 22 | 27J |

Note: the impact energy under less 50mm thickness

BeiJing ICE iron and steel co., Ltd. has been in steel industry for many years and can offer every kind of shipbuilding steel plates and steel sheets. The RINA grade B shipbuilding steel provided by Ice steel has very good quality and has been exported to worldwide shipyard and ship building company.