SAE J 403-AISI 1049 / 1050 steel plate high carbon steel 
1049 / 1050 steel plate, SAE J 403-AISI 1049 / 1050 steel plate, 1049 / 1050 high carbon steel plate and sheet, AISI steel plate, 1049 / 1050 carbon steel supplier/Chinese 1049 / 1050 steel supplier, 1049 / 1050 steel price,1049 / 1050 steel manufacturer.

1049 / 1050  steel plate is one mainly of high carbon steel,SAE J 403-AISI 1049 / 1050 steel plate is one of the higher carbon content (0.47-0.55) steels.It is equal to DIN C50,JUS Č.16301 and NF AF70C55.

| 1049 / 1050 SAE J 403-AISI Number: 1.0540 | Comparison of steel grades |
| --- | --- |
|  | JUS | Č.16301 |
|  | DIN | C50 |
|  | BS | - |
|  | GOST | - |
|  | AISI | - |
|  | UNI | - |
|  | NF | (AF70C55) |

Main chemical composition in AISI 1049 / 1050 steel : Carbon: from 0.47 to 0.55, Manganese from 0.60 to 0.90, Sulphur max 0.045, Phosphorus max 0.045, Silicon max 0.40, More detailed information, please refer to the flowing table:
Chemical Composition of 1049 / 1050 steel

| Chemical elements | C | Si max. | Mn | P max. | S max. | Cr max. | Mo max. | Ni max. | Cr+Mo+Ni max. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %, by mass | 0,47-0,55 | 0,40 | 0,60-0,90 | 0,045 | 0,045 | 0,40 | 0,10 | 0,40 | 0,63 - - |
| Permissible deviation | ± 0,02 | + 0,03 | ± 0,04 | + 0,005 | + 0,005 | + 0,05 | + 0,03 | + 0,05 |  |

1049 / 1050 high carbon steel has the good grain and Mechanical properties. It's yield strength is between 320-610 MPa ,1049 / 1050 tensile strength is from290MPa to 590MPa. More detailed information about AISI 1049 / 1050 steel Mechanical Properties , please refer to the following table:

Mechanical Properties of 1049 / 1050 steel

| Thickness of ruling section tR |
| --- |
| Diameter in mm | tR ≤ 100mm | 100< tR≤250mm | 250< tR≤500mm | 500< tR≤1000mm |
| Re min (N/mm2) | 320 | 290 | - | - |
| Rm min (N/mm2) | 610 | 590 | - | - |
| A % min. | l-longitudinal | 14 | 14 | - | - |
|  | tr -transverse | - | - | - | - |
| KV min * (J) | l-longitudinal | - | - | - | - |
|  | tr -transverse | - | - | - | - |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like SAE J 403-AISI 1049 / 1050 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  SAE J 403-AISI 1049 / 1050 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.