SAE J 403-AISI 1055 steel plate high carbon steel 
1055 steel plate, SAE J 403-AISI 1055 steel plate, 1055 high carbon steel plate and sheet, AISI steel plate, 1055 carbon steel supplier/Chinese 1055 steel supplier, 1055 steel price,1055 steel manufacturer.

1055 steel plate is one mainly of high carbon steel,UNE36011 1055 steel plate Comparison of steel grades JUS Č.1630,DIN C55, BS 070M55,GOST55 and AISI  1055 steel.

| 1055 SAE J 403-AISI Number:1.0535 | Comparison of steel grades |
| --- | --- |
|  | JIS G 4051 | S 55 C |
|  | DIN 17200 | C 55 |
|  | NFA 33-101 | AF70-C 55 |
|  | UNI 7846 | C 55 |
|  | BS 970 | 070 M 55 |
|  | UNE 36011 | C 55 k |
|  | SAE J 403-AISI | 1055 |

Main chemical composition in AISI 1055 steel : Carbon: from 0.52 to 0.60, Manganese from 0.60 to 0.90, Sulphur max 0.025, Phosphorus max 0.025, Silicon from 0.15 to 0.35, More detailed information, please refer to the flowing table:
Chemical Composition of 1055 steel

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| 1055 | 0.52-0.60 | 0.15-0.35 | 0.60-0.90 | 0.025 | 0.025 | 0.20-0.40 |

1055 high carbon steel has the good grain and Mechanical properties. It's yield strength is between 350-500 MPa ,1055 tensile strength is from550MPa to 2510MPa. More detailed information about AISI 1055 steel Mechanical Properties , please refer to the following table:

Mechanical Properties of 1055 steel

| Grade | Condition | Yield Strength R°(Mpa) | Tensile Strength Rm (Mpa) | Elongation A5(%) | Hardness HRC | Quenching Temperature (℃) | Bend ability | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| 1055 | Rolled Annealed Water-quenched Oil quenched | 500 350 | 825 550 2510 2120 | 18 30 | 61 57 | 805 845 | Min.recommended Bending radius (≤90°) | 3.0 ×t | 1.0×t |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like SAE J 403-AISI 1055 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  SAE J 403-AISI 1055 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.