SAE J 403-AISI 1060 steel plate high carbon steel 
1060 steel plate, SAE J 403-AISI 1060 steel plate, 1060 high carbon steel plate and sheet, AISI steel plate, 1060 carbon steel supplier/Chinese 1060 steel supplier, 1060 steel price,1060 steel manufacturer.

1060 steel plate is one mainly of high carbon steel,the application of SAE J 403-AISI 1060 steel plate is equal to,JIS G 4051 S 58 C,EN10083 C 60,BS970 070 M 60.

| 1060 SAE J 403-AISI Number:1.0601 | Comparison of steel grades |
| --- | --- |
|  | JIS G 4051 | S 58 C |
|  | EN10083 | C 60 |
|  | NFA 33-101 | - |
|  | UNI 7846 | - |
|  | BS 970 | 070 M 60 |
|  | UNE 36011 | - |
|  | SAE J 403-AISI | 1060 |

Main chemical composition in AISI 1060 steel : Carbon: from 0.57 to 0.65, Manganese from 0.60 to 0.90, Sulphur max 0.025, Phosphorus max 0.025, Silicon from 0.15 to 0.35, More detailed information, please refer to the flowing table:
Chemical Composition of 1060 steel

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| 1060 | 0.57-0.65 | 0.15-0.35 | 0.60-0.90 | 0.025 | 0.025 | 0.20-0.40 |

1060 high carbon steel has the good grain and Mechanical properties. It's yield strength is between 350-500 MPa ,1060 tensile strength is from550MPa to 2510MPa. More detailed information about AISI 1060 steel Mechanical Properties , please refer to the following table:

Mechanical Properties of 1060 steel

| Grade | Condition | Yield Strength R°(Mpa) | Tensile Strength Rm (Mpa) | Elongation A5(%) | Hardness HRC | Quenching Temperature (℃) | Bend ability | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| 1060 | Rolled Annealed Water-quenched Oil quenched | 500 350 | 825 550 2510 2120 | 18 30 | 61 57 | 805 845 | Min.recommended Bending radius (≤90°) | 3.0 ×t | 1.0×t |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like SAE J 403-AISI 1060 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  SAE J 403-AISI 1060 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.