SEW 083 TStE 355 TM steel plate/sheet for fine-grain structural steel

Key words: TStE 355 TM steel plate/sheet, SEW 083 TStE 355 TM steel plate/sheet, TStE 355 TM steel plate/sheet supplier/Chinese supplier, TStE 355 TM steel plate/sheet mechanical property, TStE 355 TM steel plate/sheet price.

SEW 083 TStE 355 TM steel equivalent grade:
TStE 355 TM steel plate/sheet is in SEW 083 standard, the grade number is 1.8834. The equivalent material of TStE 355 TM steel are EN10113-3 S355ML, NFA 36-201 E 355 FP, UNI 7382 Fe E 355 KTTM, BS 4360 50 EE, ASTM A 633 Gr.C.

| TStE 355TM SEW 083 Number:1.8834 | Comparision of steel grades |
| --- | --- |
|  | EN10113-3 | S355ML |
|  | NFA 36-201 | E 355 FP |
|  | UNI 7382 | Fe E 355 KTTM |
|  | BS 4360 | 50 EE |
|  | ASTM | A 633 Gr.C |

SEW 083 TStE 355 TM steel chemical composition %:
Main chemical composition in TStE 355 TM steel is carton max 0.14, silicon max 0.50, manganese max 1.6, phosphorus max 0.025, Sulphur max 0.025, chromium max 0.30. More detailed information about TStE 355 TM steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TStE355TM | 0.14 | 0.50 | 1.60 | 0.025 | 0.025 | 0.02 | 0.02 | 0.05 | 0.10 | 0.05 | 0.30 | 0.50 | 0.10 | 0.55 | 0.45 |

SEW 083 TStE 355 TM steel mechanical property:
SEW 083 TStE 355TM is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy at temperature not lower than -50 degree.

| Temperature | -50 | -40 | -30 | -20 | -10 | 0 | 20 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 27 | 31 | 40 | 47 | 51 | 55 | 63 |

| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- | --- |
| ReH-Minimun yield strength(Mpa) | 355 | 345 | 335 | 325 | 325 | 320 |

| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- |
| Rm-Tensile strength(Mpa) | 470-630 | 450-610 | 440-600 | 440-600 | 430-590 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 22 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of SEW 083 TStE 355 TM steel are available, so if need, welcome to contact ICE steel sales team.