SEW 083 TStE 420 TM steel plate/sheet for fine-grain structural steel

Key words: TStE 420 TM steel plate/sheet, SEW 083 TStE 420 TM steel plate/sheet, TStE 420 TM steel plate/sheet supplier/Chinese supplier, TStE 420 TM steel plate/sheet mechanical property, TStE 420 TM steel plate/sheet price.

SEW 083 TStE 420 TM steel equivalent grade:
TStE 420 TM steel plate/sheet is in SEW 083 standard, the grade number is 1.8836. The equivalent material of TStE 420 TM steel are EN 10113-3 S420ML, NFA 36-201 E 420 FP, 
ASTM A 633 Gr.E.

| TStE420TM SEW083 Number:1.8836 | Comparision of steel grades |
| --- | --- |
|  | EN 10113-3 | S420ML |
|  | NFA 36-201 | E 420 FP |
|  | UNI 7382 | - |
|  | BS 4360 | - |
|  | ASTM | A 633 Gr.E |

SEW 083 TStE 420 TM steel chemical composition %:
Main chemical composition in TStE 420 TM steel is carton max 0.16, silicon max 0.50, manganese max 1.7, phosphorus max 0.025, Sulphur max 0.02, chromium max 0.30. More detailed information about TStE 420 TM steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TStE420TM | 0.16 | 0.50 | 1.70 | 0.025 | 0.02 | 0.02 | 0.02 | 0.05 | 0.12 | 0.05 | 0.30 | 0.80 | 0.20 | 0.55 | 0.47 |

SEW 083 TStE 420 TM steel mechanical property:
SEW 083 TStE 420TM is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy at temperature not lower than -50 degree.

| Temperature | -50 | -40 | -30 | -20 | -10 | 0 | 20 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 27 | 31 | 40 | 47 | 51 | 55 | 63 |
| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| ReH-Minimun yield strength(Mpa) | 420 | 400 | 390 | 380 | 370 | 365 |
| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| Rm-Tensile strength(Mpa) | 520-680 | 500-660 | 480-640 | 470-630 | 460-620 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 19 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of SEW 083 TStE 420 TM steel are available, so if need, welcome to contact ICE steel sales team.