SEW 083 TStE 460 TM steel plate/sheet for fine-grain structural steel

Key words: TStE 460 TM steel plate/sheet, SEW 083 TStE 460 TM steel plate/sheet, TStE 460 TM steel plate/sheet supplier/Chinese supplier, TStE 460 TM steel plate/sheet mechanical property, TStE 460 TM steel plate/sheet price.

SEW 083 TStE 460 TM steel equivalent grade:
TStE 460 TM steel plate/sheet is in SEW 083 standard, the grade number is 1.8838. The equivalent material of TStE 460 TM steel are EN10113-3 S460M, NFA 36-201 E 460 R, UNI 7382 Fe E 460 KGTM, ASTM A 572 Gr.65.

| TStE 460 TM SEW 083 Number:1.8838 | Comparision of steel grades |
| --- | --- |
|  | EN 10113-3 | S460ML |
|  | NFA 36-201 | E 460 FP |
|  | UNI 7382 | Fe E 460 KGTM |
|  | BS 4360 | 55 EE |
|  | ASTM | A 572 Gr.65 |

SEW 083 TStE 460 TM steel chemical composition %:
Main chemical composition in TStE 460 TM steel is carton max 0.16, silicon max 0.60, manganese max 1.7, phosphorus max 0.025, Sulphur max 0.02, chromium max 0.30. More detailed information about TStE 460 TM steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TStE 460 TM | 0.16 | 0.60 | 1.70 | 0.025 | 0.02 | 0.025 | 0.02 | 0.05 | 0.12 | 0.05 | 0.30 | 0.80 | 0.20 | 0.55 | 0.48 |

SEW 083 TStE 460 TM steel mechanical property:
SEW083 TStE 460TM is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy at temperature not lower than -50 degree.

| Temperature | -50 | -40 | -30 | -20 | -10 | 0 | 20 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 27 | 31 | 40 | 47 | 51 | 55 | 63 |
| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| ReH-Minimun yield strength(Mpa) | 460 | 440 | 430 | 410 | 400 | 385 |
| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| Rm-Tensile strength(Mpa) | 540-720 | 530-710 | 510-690 | 500-680 | 490-660 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 17 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of SEW 083 TStE 460 TM steel are available, so if need, welcome to contact ICE steel sales team.