UNE 36011 C 35 k steel plate high carbon steel 
C 35 k steel plate, UNE 36011 C 35 k steel plate, C 35 k high carbon steel plate and sheet, UNE 36011 steel plate,  C 35 k carbon steel supplier/Chinese  C 35 k steel supplier,  C 35 k steel price, C 35 k steel manufacturer.

C 35 k steel plate is one mainly of high carbon steel,the application of UNE 36011 C 35 k steel plate is equal to JIS G4051 S35C,DIN17200 C 35,UNI7846  C 35,and AISI 1035.

| C35K UNE 36011 Number:1.0501 | Comparison of steel grades |
| --- | --- |
|  | JIS G 4051 | S 35 C |
|  | DIN 17200 | C 35 |
|  | NFA 33-101 | AF55-C 35 |
|  | UNI 7846 | C 35 |
|  | BS 970 | 070 M 36 |
|  | EN 10083-2 | C 35 |
|  | SAE J 403-AISI | 1035 |

Main chemical composition in UNE 36011  C 35 k steel : Carbon: from 0.32 to 0.39 , Manganese from 0.50 to 0.80, Sulphur max 0.025, Phosphorus max 0.025, Silicon from 0.15 to 0.35, More detailed information, please refer to the flowing table:
Chemical Composition of  C 35 k steel

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| C 35 k | 0.32-0.39 | 0.15-0.35 | 0.50-0.80 | 0.025 | 0.025 | 0.20-0.40 |

C 35 k high carbon steel has the good grain and Mechanical properties. It's yield strength is between 310-440 MPa ,       C 35 k tensile strength is from 480MPa to 1690MPa. More detailed information about UNE 36011  C 35 k steel Mechanical Properties , please refer to the following table:

Mechanical Properties of  C 35 k steel

| Grade | Condition | Yield Strength R° (Mpa) | Tensile Strength Rm (Mpa) | Elongation A5(%) | Hardness HRC | Quenching Temperature (℃) | Bend ability | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| C 35 k | Rolled Annealed Water-quenched Oil quenched | 440 310 | 700 480 1845 1690 | 18 30 | 53 50 | 840 880 | Min.recommended Bending radius (≤90°) | 2.0 ×t | 1.0×t |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like UNE 36011  C 35 k steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  UNE 36011  C 35 k steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.