UNE 36011 C 45 k steel plate high carbon steel 
C 45 k steel plate, UNE 36011 C 45 k steel plate, C 45 k high carbon steel plate and sheet, UNE36011 steel plate, C 45 k carbon steel supplier/Chinese C 45 k steel supplier, C 45 k steel price,C 45 k steel manufacturer.

C45K steel plate is one mainly of high carbon steel,UNE36011 C45K steel plate is under EN 10250-2:1999 standard,the material Number of C45K steel plate is 1.0503 and the comparison steel grades of C45K steel is JIS G 4051 S45C,DIN17200 C45,BS970 070M46,EN10083 C45 and SAE J403-AISI 1042/1045 steel.

| C45K UNE 36011 Number:1.0503 | Comparison of steel grades |
| --- | --- |
|  | JIS G 4051 | S 45 C |
|  | DIN 17200 | C 45 |
|  | NFA 33-101 | AF65-C 45 |
|  | UNI 7846 | C 45 |
|  | BS 970 | 070 M 46 |
|  | EN 10083-2 | C 45 |
|  | SAE J 403-AISI | 1042/1045 |

Main chemical composition in UNE36011 C 45 k steel : Carbon: from 0.42 to 0.50, Manganese from 0.50 to 0.80, Sulphur max 0.025, Phosphorus max 0.025, Silicon from 0.15 to 0.35, More detailed information, please refer to the flowing table:
Chemical Composition of C 45 k steel

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| C 45 k | 0.42-0.50 | 0.15-0.35 | 0.50-0.80 | 0.025 | 0.025 | 0.20-0.40 |

C 45 k high carbon steel has the good grain and Mechanical properties. It's yield strength is between 330-460 MPa ,C 45 k tensile strength is from 540MPa to 2270MPa. More detailed information about UNE36011 C 45 k steel Mechanical Properties , please refer to the following table:

Mechanical Properties of C 45 k steel

| Grade | Condition | Yield Strength R°(Mpa) | Tensile Strength Rm (Mpa) | Elongation A5(%) | Hardness HRC | Quenching Temperature (℃) | Bend ability | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| C 45 k | Rolled Annealed Water-quenched Oil quenched | 460 330 | 750 540 2270 1980 | 18 30 | 58 55 | 820 860 | Min.recommended Bending radius (≤90°) | 2.0 ×t | 1.0×t |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like UNE 36011 C 45 k steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  UNE 36011 C 45 k steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.