UNI 5867 Fe E 355 KGN steel plate/sheet for fine-grain structural steel

Key words: Fe E 355 KGN steel plate/sheet, UNI 5867 Fe E 355 KGN steel plate/sheet, Fe E 355 KGN steel plate/sheet supplier/Chinese supplier, Fe E 355 KGN steel plate/sheet mechanical property, Fe E 355 KGN steel plate/sheet price.

UNI 5867 Fe E 355 KGN steel equivalent material:
Fe E 355 KGN steel plate/sheet is in UNI 5867 standard, the grade material is 1.0545. The equivalent material of Fe E 355 KGN steel are UNE36081 AE355KG/AE355KW, DIN17102 STE355, NFA 36-201 E355R, EN 10111 Fe E 3555KG N.

| FeE355KGN UNI5867 MATERIAL#1.0545 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE355KG/AE355KW |
|  | DIN17102 | STE355 |
|  | NFA 36-201 | E355R |
|  | BS4036 | - |
|  | EN 10111 | Fe E 3555KG N |

UNI 5867 Fe E 355 KGN steel chemical composition %:
Main chemical composition in Fe E 355 KGN steel is carton max 0.20, silicon max 0.50, manganese max 0.90-1.65, phosphorus max 0.03, Sulphur max 0.025, chromium max 0.30. More detailed information about Fe E 355 KGN steel, please refer to the down table:

| Chemical elements | C max | Si max | Mn | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.50 | 0.90-1.65 | 0.030 | 0.025 | 0.55 | 0.30 | 0.50 | 0.12 | 0.05 | 0.02 |

UNI 5867 Fe E 355 KGN steel mechanical property:
Fe E 355 KGN steel plate is one mainly of Fine-grain structural steels, normalised rolled steel, Fe E 355 KGN steel plate under UNI5867 standard, it is normalized , fine grain structural steel.

| thickness | Yield Strength ReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | +20 KV 31J 0 KV 27J -10 KV 24J -20 KV 20J -40 - -50 - |
| t < 3mm t ≥ 3mm |  | 470-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 22 |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of UNI 5867 Fe E 355 KGN steel are available, so if need, welcome to contact ICE steel sales team.