UNI 7070 FE 590 steel plate/sheet for general Construction steels
Key words :
UNI 7070 FE 590 steel plate/sheet, UNI 7070 FE 590 steel plate/sheet, under EN standard, we can regard FE 590 steel plate/sheet for general Construction steels.UNI 7070 FE 590 steel plate/sheet is for general Construction steels. The followings are the chemical composition and the mechanical properties of EN   FE 590 steel. FE 590 steel is according to UNI 7070 standard and it is equivalent to DIN17100:St60-2,NFA: A60-2 and UNI7070:Fe590 steel grades.
Equivalent grade : 
UNI 7070 FE 590 steel plate/sheet is in UNI 7070 standard. The comparison of steel grades is: UNI 7070:1990  FE 590，DIN17100 ST60-2, NFA 35-501 A60-2,BS1449,UNI7070 FE 590.

| FE 590 UNI 7070 | Comparison of steel grades |
| --- | --- |
|  | UNI 7070:1990 | FE 590-2 |
|  | DIN17100 | ST60-2 |
|  | NFA 35-501 | A60-2 |
|  | BS1449 | - |
|  | UNI7070 | FE 590 |

FE 590 steel Chemical analysis -% by mass* 
Main chemical composition in UNI 7070 FE 590 steel : Phosphorus max 0.045, Silicon max 0.045,please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. | N max |
| --- | --- | --- | --- | --- | --- | --- | --- |
| FE 590 | - | - | - | - | 0.045 | 0.045 | 0.012 |

FE 590 steel Mechanical properties 
UNI 7070 FE 590 is general Construction steels, The different thickness with different yield strength, tensile strength and fracture elongation. More detailed information about UNI 7070 FE 590 steel Mechanical Properties , please refer to the following table:

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 335 325 |  |  | - - |
| t < 3mm t ≥ 3mm |  | 590-770 570-710 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 7 8 9 10 14 |  |

ICE steel is the professional Chinese steel exporter. We will use our professional services , best quality and competitive price to fullfill each customers needs in steel plate.