UNI 7382 Fe E 275 KGTM steel plate/sheet for fine-grain structural steel

Key words: Fe E 275 KGTM steel plate/sheet, UNI 7382 Fe E 275 KGTM steel plate/sheet, Fe E 275 KGTM steel plate/sheet supplier/Chinese supplier, Fe E 275 KGTM steel plate/sheet mechanical property, Fe E 275 KGTM steel plate/sheet price.

UNI 7382 Fe E 275 KGTM steel equivalent material:
Fe E 275 KGTM steel plate/sheet is in UNI 7382 standard, the grade number is 1.8818. he equivalent material of Fe E 275 KGTM steel are DIN StE 275 TM, UNI 10113-3 S275M.

| FeE275KGTM UNI7382 Number:1.8818 | Comparision of steel grades |
| --- | --- |
|  | DIN | StE 275 TM |
|  | UNI 10113-3 | S275M |
|  | BS 4360 | - |
|  | ASTM | - |

UNI 7382 Fe E 275 KGTM steel chemical composition % :
Main chemical composition in Fe E 275 KGTM steel is carton max 0.13, silicon max 0.50, manganese max 1.50, phosphorus max 0.025, Sulphur max 0.02, chromium max 0.30. More detailed information about Fe E 275 KGTM steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FeE275KGTM | 0.13 | 0.50 | 1.5 | 0.025 | 0.02 | 0.015 | 0.02 | 0.05 | 0.08 | 0.05 | 0.30 | 0.3 | 0.10 | 0.55 | 0.38 |

UNI 7382 Fe E 275 KGTM steel mechanical property:
Fe E 275 KGTM steel is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact UNI energy.

| Temperature | -10 | 0 | 20 |  |
| --- | --- | --- | --- | --- |
| Notch impact test. Min. absorbed UNIergy | 43 | 47 | 55 |  |
| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |  |
| ReH-Minimun yield strUNIgth(Mpa) | 275 | 265 | 255 | 245 | 245 | 240 |  |
| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| Rm-TUNIsile strUNIgth(Mpa) | 370-530 | 360-520 | 350-510 | 350-510 | 350-510 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 24 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of UNI 7382 Fe E 275 KGTM steel are available, so if need, welcome to contact ICE steel sales team.