UNI 7382 Fe E 355 KGTM steel plate/sheetfor fine-grain structural steel

Key words: Fe E 355 KGTM steel plate/sheet, UNI 7382 Fe E 355 KGTM steel plate/sheet, Fe E 355 KGTM steel plate/sheet supplier/Chinese supplier, Fe E 355 KGTM steel plate/sheet mechanical property, Fe E 355 KGTM steel plate/sheet price.

UNI 7382 Fe E 355 KGTM steel equivalent material:
Fe E 355 KGTM steel plate/sheet is in UNI 5867 standard, the grade material is 1.8823. The equivalent material of Fe E 355 KGTM steel are SEW 083 StE 355 TM, NFA 36-201 E 355 R, EN 10113-3 S355M, ASTM A 572 Gr.C.

| FeE355KGTM UNI 7382 Number:1.8823 | Comparision of steel grades |
| --- | --- |
|  | SEW 083 | StE 355 TM |
|  | NFA 36-201 | E 355 R |
|  | EN 10113-3 | S355M |
|  | BS 4360 | - |
|  | ASTM | A 572 Gr.C |

UNI 7382 Fe E 355 KGTM steel chemical composition %:
Main chemical composition in Fe E 355 KGTM steel is carton max 0.20, silicon max 0.50, manganese max 0.90-1.65, phosphorus max 0.03, Sulphur max 0.025, chromium max 0.30. More detailed information about Fe E 355 KGTM steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL min | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | Ce min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FeE355KGTM | 0.14 | 0.50 | 1.60 | 0.030 | 0.025 | 0.015 | 0.02 | 0.05 | 0.10 | 0.05 | 0.30 | 0.50 | 0.10 | 0.55 | 0.39 |

UNI 7382 Fe E 355 KGTM steel mechanical property:
FeE355KGTM is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy.

| Grade | Nom. thick.e | Yield Strengh ReH | Tensile Strength ReH | Total Elongation A5 | ℃ | Notch Impact Energy Longitud. transverse |
| --- | --- | --- | --- | --- | --- | --- |
| FeE355KGTM | ≤16mm | ≥355MPa | 470- 630 MPa |  | +20 | ≥55 | ≥31 |
|  | ＞16mm | ≥345MPa |  |  | 0 | ≥47 | ≥27 |
|  | ≥3mm |  |  | ≥22% | -10 | ≥43 | ≥24 |
|  |  |  |  |  | -20 | ≥40 | ≥20 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of UNI 7382 Fe E 355 KGTM steel are available, so if need, welcome to contact ICE steel sales team.