UNI 7382 Fe E 460 KTTM steel plate/sheet for fine-grain structural steel

Key words: Fe E 460 KTTM steel plate/sheet, UNI 7382 Fe E 460 KTTM steel plate/sheet, Fe E 460 KTTM steel plate/sheet supplier/Chinese supplier, Fe E 460 KTTM steel plate/sheet mechanical property, Fe E 460 KTTM steel plate/sheet price.

UNI 7382 Fe E 460 KTTM steelequivalent material:
Fe E 460 KTTM steel plate/sheet is in UNI 7382 standard, the grade number is 1.8838. he equivalent material of Fe E 460 KTTM steel are SEW 083 TStE 460 TM, NFA 36-201 E 460 FP, EN10113-3 S460ML, BS 4360 55 EE, ASTM A 572 Gr.65.

| FeE460KGTM UNI7382 Number:1.8838 | Comparision of steel grades |
| --- | --- |
|  | SEW 083 | TStE 460 TM |
|  | NFA 36-201 | E 460 FP |
|  | EN10113-3 | S460ML |
|  | BS 4360 | 55 EE |
|  | ASTM | A 572 Gr.65 |

UNI 7382 Fe E 460 KTTM steel chemical composition %:
Main chemical composition in Fe E 460 KTTM steel is carton max 0.16, silicon max 0.60, manganese max 1.70, phosphorus max 0.025, Sulphur max 0.02, chromium max 0.30. More detailed information about Fe E 460 KTTM steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S420ML | 0.16 | 0.60 | 1.70 | 0.025 | 0.02 | 0.025 | 0.02 | 0.05 | 0.12 | 0.05 | 0.30 | 0.80 | 0.20 | 0.55 | 0.48 |

UNI 7382 Fe E 460 KTTM steel mechanical property:
FeE460KGTM is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy at temperature not lower than -50 degree.

| Temperature | -50 | -40 | -30 | -20 | -10 | 0 | 20 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 27 | 31 | 40 | 47 | 51 | 55 | 63 |
| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| ReH-Minimun yield strength(Mpa) | 460 | 440 | 430 | 410 | 400 | 385 |
| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| Rm-Tensile strength(Mpa) | 540-720 | 530-710 | 510-690 | 500-680 | 490-660 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 17 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of UNI 7382 Fe E 420 KTTM steel are available, so if need, welcome to contact ICE steel sales team.