DIN17102 WSt 285 steel plate/sheet for Boilers and Pressure Vessels
Key words :
WSt 285 steel plate/sheet, DIN17102 WSt 285 steel plate/sheet, DIN17102 WSt 285 steel plate/sheet for Boilers and Pressure Vessel steel, WSt 285 steel plate/sheet for Boilers and Pressure Vessel, DIN17102 steel plate for Boilers and Pressure Vessel using, WSt 285 steel supplier/Chinese supplier, WSt 285 steel price...

Equivalent grade :
WSt 285 steel plate/sheet is in DIN17102 standard. The equal material of WSt 285 steel is: EN 10028-2 P275NH,  NFA 36-205  A 42 CP,AP,FP

| WSt 285 DIN17102 | Comparison of steel grades |
| --- | --- |
|  | EU 113 | - |
|  | NBN629 | - |
|  | EN 10028-2 | P275NH |
|  | NFA36205 | A 42 CP,AP,FP |

DIN17102 WSt 285 steel Chemical Composition % : 
Main chemical composition in DIN17102 WSt 285 steel: Carbon Max 0.16, Manganese from 0.08 to 1.50, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.40, More detailed information, please refer to the flowing table:

DIN17102 WSt 285 steel  steel Chemical Composition %

| Grades | C max | Si max | Mn. max | P max | S max | N max | AL min | Cr max | Cu max | Mo max | Ni max | Nb max | Ti max | V max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| WSt 285 | 0.16 | 0.40 | 0.80-1.50 | 0.025 | 0.015 | 0.012 | 0.020 | 0.300 | 0.30 | 0.08 | 0.50 | 0.05 | 0.03 | 0.05 |

DIN17102 WSt 285 steel Mechanical Properties
WSt 285 this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 215- 275 MPa (there is different min strength point at the different thickness.) WSt 285 tensile strength is from 350MPa to 510MPa. (different min strength point at the different thickness.) More detailed information about DIN17102 WSt 285 steel Mechanical Properties , please refer to the following table:

| Grade | Thickness ( mm) | Yield Strength MPa(min) | Tensile Strength MPa | Elongation % (min) |
| --- | --- | --- | --- | --- |
| WSt 285 | ≤ 16 | 275 | 390 to 510 | 24 |
|  | 16＜t ≤40 | 265 | 390 to 510 | 24 |
|  | 40＜t ≤60 | 255 | 390 to 510 | 24 |
|  | 6＜t ≤100 | 235 | 370 to 490 | 23 |
|  | 100＜t ≤150 | 225 | 360 to 480 | 23 |
|  | 150＜t ≤250 | 215 | 350 470 | 23 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.